|  | SIL BLUE 7010 (STD) |
| --- | --- |
|  | PRODUCT; SIL BLUE 7010 (STD). C.I. NAME; COPPER PHTHALOCYANINE (CRUDE) BLUE.. Trade Name; CPC. Molecular Wt.; 575.5. Molecular Formula; C32H16N8Cu. Physical Appearance; Blue Powder. PHYSICAL PROPERTIES. Purity; Min. 97 %. Bulk Density; 0.5 Gms/cc. Conductivity; Less than 250 M. Mhos. pH; 6.5 - 7. Total Cu. Cont.; More than 10.7 %. Free Cu.; Less than 125 PPM. PCB Content; nil. Inflammability; Absent. Nuisance Value; By Colour - Yes By Odour - No. Grit Cont.; Not More than 100 PPM. Decomposition; Above 3300 C.. Mesh Size; 100 % above 250 mesh. IMPURITIES IN CPC. Volatile Matter; Less than 0.5 %. Acid Soluble impurities; Traces. Alkali Soluble Impurities; Less than 0.5 % (In 5 % NaOH). PACKING. Sea worthy 25 kgs HDPE bags/500 kgs PP bags with polythene liners.. APPLICATIONS. CPC Blue Crude is the main raw material used in the manufacture of pigments such as Pigment Green 7, Pigment Alpha Blue, Pigment Beta Blue etc. It is also used in the manufacture of a number of Reactive & Direct Dyes.. Note : This product dose note contain colophony... |